PUBLIC PROTECTION CABINET

Department of Housing, Buildings and Construction

Division of Plumbing
(Amendment)
815 KAR 20:060. Quality and weight of materials.

RELATES TO: KRS 318.130, 318.150, 42 U.S.C. 300g-6(d)(2)

STATUTORY AUTHORITY: KRS 198B.040(10), 318.130

NECESSITY, FUNCTION, AND CONFORMITY: KRS 318.130 requires the department[, after review by the State Plumbing Code Committee,] to promulgate an administrative regulation establishing the Kentucky State Plumbing Code to regulate [regulating] plumbing, including the quality and weight of material. This administrative regulation establishes the manufacturer's specification number for the quality and weight of material that shall be used in the installation of plumbing systems and establishes minimum specifications for the intended use.

Section 1. Definitions. (1) “ASME” means the American Society of Mechanical Engineers.
(2) "CISPI" means the Cast Iron Soil Pipe Institute. 
(3) "Lead" means solders and flux containing more than two-tenths (0.2) percent lead and the wetted surfaces of pipes, pipe fittings, plumbing fittings, and fixtures containing more than a weighted average of 0.25 percent lead as calculated according to the formula established in 42 U.S.C. 300g-6(d)(2). ["ABS" means acrylonitrile-butadiene-styrene.

(2) "ASTM" means American Society for Testing and Materials and copies of specifications identified in this administrative regulation can be obtained by writing the American Society for Testing and Materials, 1916 Race Street, Philadelphia, Pennsylvania 19103.

(3) "CISPI" means the Cast Iron Soil Pipe Institute and copies of specifications identified in this administrative regulation can be obtained by writing the Cast Iron Soil Pipe Institute, 5959 Shallowford Road, Suite 419, Chattanooga, TN 37421.

(4) "Lead" means solders and flux containing more than two-tenths (0.2) percent lead and the wetted surfaces of pipes, pipe fittings, plumbing fittings, and fixtures containing more than a weighted average of one quarter (0.25) percent lead as calculated according to the formula established in 42 U.S.C. 300g-6(d)(2).

(5) "PVC" means polyvinyl chloride.]
Section 2. Quality of Materials. The material used in a drainage or plumbing system or part of a system shall be free of defects.

Section 3. Label, Cast, or Stamped. Each length of pipe, fitting, trap, fixture, or device used in a plumbing or drainage system shall be stamped or indelibly marked with the:

(1) Weight or quality; and

(2) Maker's mark or name (manufacturer's specification number).

Section 4. Vitrified clay pipe, concrete pipe, truss pipe, and extra heavy SDR 35 sewer piping shall be produced, labeled, and used only as established in subsections (1) through (4) of this subsection.

(1) Vitrified clay pipe shall be as established in ASTM C-700.

(2) Concrete pipe shall be as established in ASTM C-14.

(3)(a) Except as established in paragraph (b) of this subsection, truss pipe shall be as established in ASTM D-2680. 
(b) Solid wall truss pipe shall be as established in ASTM D2751.

(4) Extra heavy SDR 35 sewer piping shall be as established in ASTM D-3033-74 and D-3034-74.

Section 5. Cast-iron Pipe. (Hub and Spigot and No-hub). (1) Extra heavy. Extra heavy cast-iron pipe and fittings shall be produced and labeled as ASTM A74.

(2) Service-weight. Service-weight cast-iron pipe and fittings shall be produced and labeled as ASTM A74 and C1563.

(3) No-hub cast-iron and fittings shall be produced and labeled ASTM 888 or CISPI 301.

(4) No-hub couplings shall be produced and labeled as ASTM C1277, C564, C1563, or CISPI 310.

(5) Coating. Cast-iron pipe and fittings for underground use shall be coated with:

(a) Asphaltum;

(b) Coal tar pitch; or

(c) A coating produced and labeled as ASTM A743.

Section 6. Wrought-iron Pipe. All wrought-iron pipe shall be produced and labeled with the latest ASTM "specifications for welded wrought iron pipe".

Section 7. Mild-steel Pipe. Steel pipe shall be produced and labeled with the latest ASTM "specifications for welded and seamless steel pipe".

Section 8. Brass Pipe; Copper Pipe; and Brass Tubing. Brass pipe, copper pipe, and brass tubing shall be produced and labeled with the latest specifications of ASTM for "brass pipe, copper pipe, and brass tubing, standard sizes".

Section 9. Borosilicate Pipe, Plastic Pipe, Stainless Steel Tubing, Polyethylene Pipe, and Polypropylene Pipe. (1) Borosilicate pipe. Borosilicate pipe shall be produced and labeled with the latest ASTM specifications.

(2) Plastic pipe. All plastic piping used in a drainage, waste, and vent system shall be:

(a) Schedule 40 or 80, Type 1, Grade 1, polyvinyl chloride produced and labeled as ASTM D1784;

(b) Cellular core PVC produced and labeled ASTM F-891;

(c) Schedule 40 or 80 acrylonitrile-butadiene-styrene produced and labeled as ASTM D2661; or

(d) Cellular core ABS produced and labeled as ASTM F-628.

(3) Pipe and fittings shall be produced and labeled in accordance with the provisions of ASTM-D-2665, as amended, for PVC and ASTM-D-2661 for ABS, and both shall bear the National Sanitation Foundation seal of approval.

(4) Copies of National Sanitation Foundation specifications for the manufacture of products identified in this administrative regulation may be obtained by writing the National Sanitation Foundation (NSF), 3475 Plymouth Road, P.O. Box 1468, Ann Arbor, MI 48106.

(5) All pipe and fittings shall bear the ASTM designation together with the NSF seal, the manufacturer's identification, and the size.

(6)(a) Except as established in paragraph (b) of this subsection, the use of plastic pipe and fittings (PVC or ABS) shall be limited to buildings in which the plumbing system does not exceed forty-five (45) feet in height, measured from the grade plane [as defined by the Kentucky Building Code, 815 KAR 7:120, or Kentucky Residential Code, 815 KAR 7:125], and continuing through the vertical distance of the building to a maximum height of forty-five (45) feet.

(b) Plastic pipe and fittings may be installed in a building in which the plumbing system exceeds forty-five (45) feet in height if the installation complies with all of the requirements established in subparagraphs 1. through 3. [8.] of this paragraph.

1. The use of PVC and ABS piping shall be limited to schedule 40 or 80 produced and labeled as ASTM D2665 and D1784 for PVC piping and ASTM D2661 for ABS piping.

2.  The installation of the plastic pipe and fittings (PVC or ABS) shall be made in compliance with the manufacturer’s recommendations, which shall be made available to the inspector. 
3.  Firestop systems shall be inspected in accordance with ASTM E2174 by an approved inspection agency. [The building shall not have an occupied floor located more than seventy-five (75) feet above the lowest level of fire department vehicle access.
2. Detailed building elevation plans shall be submitted to the department for any building exceeding forty-five (45) feet in height.

3. The use of plastic pipe and fittings (PVC or ABS) shall be limited to a vertical distance of forty-five (45) feet within the plumbing system, measured from the terminus of the plumbing system as it passes through the roof and continuing down the plumbing system to a maximum distance of forty-five (45) feet.

4. The use of plastic pipe and fittings (PVC or ABS) shall be allowed for use in the installation of the plumbing system located below ground underneath a building. Once the underground piping first penetrates the floor or slab, the plastic pipe shall be transitioned to other approved materials listed in 815 KAR 20:090 within six (6) inches of the floor or slab through which it penetrates.

5. The use of polyvinyl chloride and acrylonitrile-butadiene-styrene piping shall be limited to schedule 40 or 80 produced and labeled as ASTM D2665 and D1784 for PVC piping and ASTM D2661 for ABS piping.

6. The installation of the plastic pipe and fittings (PVC or ABS) shall be made in compliance with the manufacturer’s recommendations, which shall be made available to the inspector.
7. All plastic (PVC or ABS) vertical drain, waste, and vent stacks shall be protected in a shaft enclosure constructed in accordance with the Kentucky Building Code, 815 KAR 7:120, or Kentucky Residential Code, 815 KAR 7:125.

8. All plastic pipe penetrations in the shaft enclosure shall be protected as required by the Kentucky Building Code, 815 KAR 7:120, or Kentucky Residential Code, 815 KAR 7:125.]
 (7) Stainless steel tubing.

(a) Stainless steel tubing for hot and cold water piping shall be [Grade H] produced and labeled either as ASTM A269 or ASTM A312 [A268/268M].

(b) Stainless steel tubing for the soil, waste, and vent system shall be 316L [either Grade G or H] produced and labeled as ASME A112.3.1 [ASTM A268/268M].

(8) [Polyethylene pipe.] Polyethylene pipe used in acid waste systems shall be produced and labeled as ASTM D-1204.

(9) [Polypropylene pipe.] Polypropylene pipe used in acid waste systems shall be produced and labeled as ASTM D-4101 or ASTM F-1412.

Section 10. Lead Pipe, Diameter, Weights. (1) Lead soil, waste, and vent pipe shall be produced and labeled as Federal Specifications WW-P-325 and shall not be lighter than the weights established in the following table:

	Size 

Inside Diameter Inches
	Commercial Designation "D" or "XL"
	Wall Thickness Inches
	Weight Pounds
	Per Foot Ounces

	1 1/2
	D
	XL
	0.138
	3
	8

	2
	D
	XL
	0.142
	4
	12

	3
	D
	XL
	0.125
	6
	0

	4
	D
	XL
	0.125
	8
	0

	
	
	
	
	
	
	


(2) Lead bends and lead traps. All lead bends and lead traps shall be of the weight known as extra heavy (XH) and shall have at least one-eighth (1/8) inch wall thickness.

Section 11. Integral Flashing. If a roofing system requires integral flashing, a flashing material, which is part of the manufactured roofing system and required by the roofing manufacturer to guarantee or warranty the roofing system, shall be used.

Section 12. Sheet Lead. Sheet lead for a shower pan shall not weigh less than four (4) pounds per square foot and shall not weigh less than two and one-half (2 1/2) pounds per square foot for vent pipe flashings.

Section 13. Sheet Copper or Brass. Sheet copper or brass shall not be lighter than No. 18 B. & S. gauge, except local and interior ventilating pipe shall not be lighter than No. 26 B. & S. gauge.

Section 14. Threaded Fittings. (1) A plain screw fitting shall be either cast-iron, malleable iron, or brass of standard weight and dimension.

(2) A drainage fitting shall be either cast-iron, malleable iron, or brass, with smooth interior waterway, with threads tapped out of solid metal.

(3) A cast-iron fitting used in a water supply distribution shall be galvanized.

(4) A malleable iron fitting shall be galvanized.

Section 15. Caulking Ferrules. A caulking ferrule shall be of red brass and shall be in accordance with the following table:

	Pipe Sizes

Inches
	Inside Diameter Inches
	Length

Inches
	Minimum

Weight Each

	2
	2 1/4
	2 1/2
	1 lb. 0 oz.

	3
	3 1/4
	4 1/2
	1 lb. 12 oz.

	4
	4 1/4
	4 1/2
	2 lb. 8 oz.


Section 16. Soldering Nipples. A soldering nipple shall be recessed red cast brass, iron pipe size. If cast, they shall be full bore and of minimum weight.

Section 17. Floor Flanges for Water Closets and Service Sinks or Similar Fixtures. (1) A floor flange shall either be:

(a) Hard lead;

(b) Brass;

(c) Cast iron;

(d) Galvanized malleable iron;

(e) ABS; or

(f) PVC.

(2) A hard lead or brass flange shall not be less than one-eighth (1/8) inch thick.

(3) Cast iron or galvanized malleable iron shall:

(a) Not be less than one-fourth (1/4) inch thick; and

(b) Have a two (2) inch caulking depth.

Section 18. Use of Lead. (1) Lead shall not be used in the installation or repair of a public or private water system providing potable water for human consumption.

(2) This section shall not apply to:

(a) Pipes, pipe fittings, plumbing fittings, or fixtures, including backflow preventers, that are used exclusively for nonpotable services such as manufacturing, industrial processing, irrigation, outdoor watering, or any other uses in which the water is not anticipated to be used for human consumption; or

(b) Toilets, bidets, urinals, fill valves, flushometer valves, tub fillers, shower valves, service saddles, or water distribution main gate valves that are two (2) inches in diameter or larger.

Section 19. New Materials. (1) Materials other than those established in this administrative regulation shall be prohibited unless the material is specifically approved by the [State Plumbing Code Committee and the] department [of Housing, Buildings and Construction] as being equal to or better than the material specified in the State Plumbing Code.

(2) It shall be the responsibility of any person or company seeking the approval of a material not included in this code to prove that the material is equal to or better than the material that it is intended to replace.

(3) Procedural requirements for approval of new parts and materials are established in 815 KAR 20:020.
____________



______________________________

       DATE




STEVEN A. MILBY, COMMISSIONER

DEPARTMENT OF HOUSING, BUILDINGS

                                                         
AND CONSTRUCTION

____________



______________________________

       DATE




DAVID A. DICKERSON, SECRETARY







PUBLIC PROTECTION CABINET
















 
PUBLIC HEARING AND PUBLIC COMMENT PERIOD: A public hearing on this administrative regulation shall be held on October 25, 2016, at 9:00 a.m., EDT, at the Department of Housing, Buildings and Construction, 101 Sea Hero Road, Suite 100, Frankfort, Kentucky. Individuals interested in being heard at this hearing shall notify this agency in writing by five working days prior to the hearing of their intent to attend.  If no notification of intent to attend the hearing is received by that date, the hearing may be canceled.  The hearing is open to the public.  Any person who wishes to be heard will be given an opportunity to comment on the proposed administrative regulation.  A transcript of the public hearing will not be made unless a written request for a transcript is made.  If you do not wish to be heard at the public hearing, you may submit written comments on the proposed administrative regulation.  Written comments shall be accepted through October 31, 2016. Send written notification of intent to be heard at the public hearing or written comments on the proposed administrative regulation by the above date to the contact person:

CONTACT PERSON:
Tim Cocanougher, Office of the General Counsel





Department of Housing, Buildings and Construction





101 Sea Hero Road, Suite 100





Frankfort, Kentucky 40601-5412





Telephone:  502-573-0365 





FAX:  502-573-1057





tim.cocanougher@ky.gov

REGULATORY IMPACT ANALYSIS

AND TIERING STATEMENT
Administrative Regulation:
815 KAR 20:060
Contact person:  


Tim Cocanougher
Phone Number:


(502) 573-0365

Email:



tim.cocanougher@ky.gov
(1)
Provide a brief summary of:  

(a)
What this administrative regulation does: This administrative regulation establishes the waste pipe size requirements for various plumbing fixtures and appurtenances for buildings in Kentucky.
(b) The necessity of this administrative regulation: This administrative regulation is necessary to implement the Division of Plumbing’s statutory duty to establish a state plumbing code that regulates the construction, installation, and alteration of plumbing and plumbing fixtures and appliances, house sewers, and private water supplies, including the size of waste pipes.
(c)
How this administrative regulation conforms to the content of the authorizing statutes: KRS 318.130 requires the department to promulgate an administrative regulation to establish the Kentucky State Plumbing Code, which will regulate plumbing, including waste pipes for plumbing fixtures and appurtenances.
(d)
How this administrative regulation currently assists or will assist in the effective administration of the statutes:  This administrative regulation assists the Division of Plumbing establish the size of waste pipes needed for various fixtures in buildings in Kentucky.

(2) If this is an amendment to an existing administrative regulation, provide a brief summary of:

 


(a)
How the amendment will change this existing administrative regulation:    This amendment allows additional material (PVC or ABS) to be used in the plumbing system for buildings that exceed 45 feet in height.





(b)
The necessity of the amendment to this administrative regulation:  This amendment is necessary to expand upon the permissible types of materials used in a plumbing system.



(c)
How the amendment conforms to the content of the authorizing statutes:   This amendment directly relates to the permissible types of material used in a plumbing system.



(d)
How the amendment will assist in the effective administration of the statutes: This amendment will provide greater flexibility in designing plumbing systems, and bring Kentucky into conformity with surrounding states and the majority of the country.
(3) List the type and number of individuals, businesses, organizations, or state and local governments affected by this administrative regulation:  All individuals engaged in designing and the installation of plumbing in buildings that exceed 45 feet in height within the Commonwealth, as well as all owners and operators of buildings in which the plumbing materials described in this regulation are required or otherwise installed.
(4)
Provide an analysis of how the entities identified in question (3) will be impacted by either the implementation of this administrative regulation, if new, or by the change, if it is an amendment, including;


(a)
List the actions that each of the regulated entities identified in question (3) will have to take to comply with this administrative regulation or amendment:  This amendment allows designers and owners more options when selecting materials for their projects, so no actions will be required.

(b)
In complying with this administrative regulation or amendment, how much will it cost each of the entities identified in question (3):  Affected entities could anticipate decreased expenses for new installations of plumbing because this amendment increases the types of materials allowed in a plumbing system.


(c)
As a result of compliance, what benefits will accrue to the entities identified in question (3):  Benefits include additional material options for plumbing installations, making the installation of plumbing more consistent with other states.
(5)
Provide an estimate of how much it will cost to implement this administrative regulation:


(a)
Initially:   There are no anticipated additional costs to administer this amendment.


(b) 
On a continuing basis:  There are no anticipated additional costs to administer this amendment.

(6)
What is the source of the funding to be used for the implementation and enforcement of this administrative regulation:   Implementation of this amendment is not anticipated to result in additional costs to the agency.  Any agency costs resulting associated with this amendment will be met with existing agency funds.
(7)
Provide an assessment of whether an increase in fees or funding will be necessary to implement this administrative regulation, if new, or by the change if it is an amendment:   This amendment will not necessitate an increase in fees or require funding from the Department for implementation.  

(8)
State whether or not this administrative regulation establishes any fees or directly or indirectly increases any fees:  There are no fees increased by this amendment.

(9)
TIERING: Is tiering applied? (Explain why tiering was or was not used.)  Tiering is not applied.  This administrative regulation applies with equal force to all buildings in which the plumbing system exceeds forty-five (45) feet in height.
FISCAL NOTE ON STATE OR LOCAL GOVERNMENT

Regulation No.  
815 KAR 20:060
Contact Person:  
Tim Cocanougher
Phone Number:
(502) 573-0365
Email:

tim.cocanougher@ky.gov

1. What units, parts or divisions of state or local government (including cities, counties, fire departments, or school districts) will be impacted by this administrative regulation?  The Department of Housing, Buildings and Construction, Division of Plumbing.


2. Identify each state or federal statute or federal regulation that requires or authorizes the action taken by the administrative regulation.  This regulation is authorized by KRS 318.130.  

3. Estimate the effect of this administrative regulation on the expenditures and revenues of a state or local government agency (including cities, counties, fire departments, or school districts) for the first full year the administrative regulation is to be in effect.  


(a) How much revenue will this administrative regulation generate for the state or local government (including cities, counties, fire departments, or school districts) for the first year?  This amendment is not anticipated to generate additional revenues for the agency.


(b) How much revenue will this administrative regulation generate for the state or local government (including cities, counties, fire departments, or school districts) for subsequent years?  This amendment is not anticipated to generate additional revenues for the agency.



(c) How much will it cost to administer this program for the first year?  There are no anticipated additional costs to administer this regulatory amendment.


(d) How much will it cost to administer this program for subsequent years?  There are no anticipated additional costs to administer this regulatory amendment.

Note: If specific dollar estimates cannot be determined, provide a brief narrative to explain the fiscal impact of the administrative regulation.


Revenues (+/-):  
Neutral

Expenditures (+/-): 
Neutral

Other Explanation: 
Neutral
1

